# Washstand Trigo Comfort made from the copolymer-bound mineral material VARICOR® (material in accordance to ISO norm 19712). Homogeneous, coloured throughout, pore-free material, without surface sealing like gel coat or glaze, largely resistant against disinfectants and commonly-used chemicals, heat resistant against burning cigarette, standard plain white colour shades (arktis, white-alpine) have good antibacterial properties in accordance to ISO 22196 (other colours on request). Optionally available with antiviral properties.

**Single washstand** moulded to order in one piece, **multiple washstand** made of several single washstands bonded together seamlessly and ready made-up, with side shelves, machinable on site, with rectangular basin sloping towards the easily accessible drain channel, with direct transition to the drain opening, standard with overflow, optional tap hole, with skirt, with chamfered wall-connection profile, with back rim for hanger bolt fastening.

**Trigo Comfort** qualifies for CE marking in compliance with DIN EN 14688.

Internal basin dimensions (L x W x D): 500 x 400 x 90 mm

Depth: 520 mm

Material thickness: 12 mm

Skirt: H = 180 mm

Chamfered wall-connection profile: H = 30 mm

Length of single washstand: 700 – 2500 mm

Length of multiple washstand: from 1400 mm

Attachment: Hanger bolts (included)

 480-mm wall-mounting bracket for alcove installation

 (available as additional accessories)

Accessories (optional): • 480 mm wall-mounting bracket for alcove installation

 • Connection piece for trap included

Optional features: • Side section, seamlessly bonded left and/or right

 • Functional cut-out (e.g. towel holder)

 • Paper waste tube (round or rectangular), seamlessly

 bonded

**Model: Trigo Comfort**

**Distribution via: VARICOR GmbH**

 **Waldstr. 33**

 **76571 Gaggenau (Germany)**

 **Tel.: +49 (0) 7225/9739-0**

[www.varicor.com](http://www.varicor.com)